## Slide 1: An Accurate Coarse Grained Model for Polysaccharides In Solution
Levan Tsereteli, Dr. Andrea Grafmueller

## Slide 2
Bottom-up Coarse Graining
Quantum Mechanics – 100-200 Atoms
- MD parameters with Amber GLYCAM protocol
- QM/MD
MD and Metadynamic Simulations – - Atoms
Monte Carlo Simulations – Billions of Atoms
Code Development for polymer Sampling and interaction with various surfaces
Close to real Experimental System Size

## Slide 3
= + +
= 4 + T +
  =
= Tln(10)(pH - p)
Force-Field For the Pivot Move MC
Force-Field For the Titration MC
Our model is based on an improved version of the Pivot Move Markov Chain Monte Carlo sampling method, which leads to a more precise description of the system. Nine types of glycosidic linkages can be found for Chitosan. PMFs are visually similar however differ by total accessible angular space, width and depth of the corresponding minima.
That small difference highly effects mechanical properties of the polymer. After protonation MC PMFs along the polymer are updated.
PMF Specific Persistence Length

## Slide 4
Model showed to be highly accurate for the polymers in a good solvent, where electrostatic interaction is predominant. Depending on the conditions of the solvent pH and Ionic Strength (Cs) stiffness of the polymer varies covering wide range of the experimental findings.
Experimental Conditions | Simulations | Experiment | Diff.
2100 Units, DD = 91 % | 76.718 nm | 82.5 nm | -7.0 %
1500 Units, DD = 91 % | 62.516 nm | 58.5 nm | 6.8 %
1000 Units, DD = 91 % | 51.072 nm | 47.4 nm | 7.7 %
305 Units, DD = 91 % | 23.534 nm | 26 nm | -9.8 %
711 Units, DD = 80 % | 36.646 nm | 41 nm | -10.6 %
694 Units, DD = 70 % | 33. 701 nm | 39 nm | -13.58 %
Considering polydispersity of the Chitosan polymers in solution, experimental values for the radius of gyration is recovered as closely as was expected. Titration curves are recovered with close to 100 % accuracy.

## Slide 5
pH 1
pH 3
pH 7
SUV Dimeter 10 nm; DD 80 %; DOPC/DOPG ratio 3/7; Cs 0.1
DOPC head group
DOPG negatively charged head group
DOPG neutral head group
Adsorption of Chitosan on
Liposomes – Fully titratable model
Neutral Chitosan Monomer
Protonated Chitosan Monomer